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Figure 51. 2619_2626 TRACE VIN               Figure 52. 2619_2626 POWER VIN
Date Code: 2619+2626:                       Date Code: 2619+2626: 
Before apply 12V between VIN and GND          Apply 12V between VIN and GND
Passed                                     Failed 
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Figure 53. 2619_2626 TRACE VIN BURNT                 Figure 54. 2626 TRACE VIN
Date Code: 2619+2626:                      Date Code: 2626: 
After applied 12V between VIN and GND        Before apply 12V between VIN and GND
Curve Trace result Failed and show shorted.      Passed 
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Figure 55. 2626 POWER VIN                    Figure 56. 2626 TRACE VIN BURNT
Date Code: 2626:                             Date Code: 2626:
Apply 12V between VIN and GND                After applied 12V between VIN and GND 
Failed                                      Curve Trace result Failed and show shorted. 
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Figure 57. 2629 TRACE VIN                   Figure 58. 2629 POWER VIN
Date Code: 2629:                           Date Code: 2629: 
Before apply 12V between VIN and GND        Apply 12V between VIN and GND 
Passed                                   Failed
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Figure 59. 2629 TRACE VIN BURNT 
Date Code: 2629: 
After applied 12V between VIN and GND 
Curve Trace result Failed and show shorted. 
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Analysis Report - 6000-9758

@ Customer Name: | == = Purchase Order: | 11052
N 5 Part Number: | TPS5420DR Customer P/N: [ NOT AVAILABLE
GLOBAL ETS Manufacturer: | TEXAS INSTRUMENTS Devices Received: | 20,000

Date Code: | 2619/2626, 2626/2629, 2626, 2629 Lot Code: [ Not Applicable

5.0.0 | Electrical - Curve Trace Testing, at ambient temp. - 10 Devices per date code (MiL-STD-883) (Non-Destructive)

Results Summary
Curve tracing test was performed on 1 samples per date code. Total 3pcs devices were tested. Devices supply pins were failed after applied typical voltage. The

VIN and GND pins of all devices are shorted after applied typical voltage.

Quantity

Inspected | Pass | Fail | NA Comments / Observations

‘Test-Process Operation

5.1.0 | Electrical Test (MIL-STD-883, (AS6171/7) (Non-Destructive)

5.1.1 | Curve Trace Test TA = 25°C 3 0 -

Equipment Used | NI VIRTUAL BENCH  AssetTag: 19 Calibration Due Date: 2027-01-01  Cert: RF260001

Images For Electrical - Curve Trace Testing, at ambient temp. - 10 Devices per date code.

BOOT PH
NC VIN
NC GND
VSENSE ENA

Figure 4-1. D Package, 8-Pin SOIC (Top View)

Figure 50. PIN DIAGRAM
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