MC33078P Burn-in result:
A total of 840 pcs of IC in 210 boards (each board contains 4 ICs) are burned in and the result is as follows:
	Day
	No of ICs failed
	Cumulative No. of ICs failed

	1
	4
	4

	2
	2
	6

	3
	2
	8

	4
	0
	8

	5
	2
	10



Failure symptom: Supplies to +15V and -15V are fused.
Failure analysis: Pin 8 (VCC+) and Pin 4 (VCC-) of the IC are shorted as compared to other good IC.
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Illustrative burn-in circuit:
[image: ]





image1.png
RI0 R20

o ot

Rit Ris i

ot ot L
GEY

s

Mcsors pirs





