## Slide 1: PAL Overview

## Slide 2: Introduction
In the late 70s a few design engineers got together and decided to shrink a circuit board onto a single chip. They wanted to make it so the customer could do the same thing. But most customers don’t want to pay the cost of a set of reticles and the associated development time and cost.

## Slide 3: Let’s Blow a Fuse!
There happened to be a power engineer on the team and he/she remembered how easy it was to separate a conductor. Idea! “Let’s vaporize metal under the protective overcoat -- in the presence of other metals, oxides, and silicates.”
So they did!!

## Slide 4: Sometimes There Was Overblow!

## Slide 5: Sometimes There Was Underblow

## Slide 6: They Finally Learned to Control It -- Sort Of!

## Slide 7: Today We Live With the Results

## Slide 8: Overview of PAL Devices
Definition
Architecture
  ALS
  Zener Heavy

## Slide 9: PAL Definition
PAL and PLD are synonymous. Both of them refer to an array of logic that can be programmed using fuses to implement a circuit of combinatorial logic or registered logic.
PAL is an AMD registered trademark meaning Programmable Array Logic.
PLD is the generic name which stands for Programmable Logic Device.

## Slide 10: PAL Uses
PALs were probably the first ASIC (Application Specific Integrated Circuit) type devices available. A previous design of an entire circuit board consisting of logic components could be implemented on one chip.
They are field-programmable. The customer buys a blank part and uses a programmer to implement the circuit that he has designed. If it does not function they way he expected, it is a simple matter to change it quickly and check the revisions.

## Slide 11: PAL Uses (Cont’d)
The same type parts used for prototype development can then be used in production.
Later, revisions to the full-up system that require changes to the PAL design are easily implemented.

## Slide 12: PAL Architecture
Most of TI’s PALs are Bipolar. They are built with two processes:
  Impact -- An ALS process that is older but more stable. These are still being built in SFAB. PALs made from this process are the ones that Sherman FA will see the most.
  Impact-X -- A bipolar process that was used in HFAB. The process was faster but less stable. This process was not moved to SFAB, and PALs are no longer manufactured using Impact-X. We still have a large die bank from which parts are being assembled and sold.

## Slide 13: PAL Architecture (Cont’d)
  CMOS -- This FAMOS process was used in LMOS. These contain no fuses. They use an EPROM technology to implement the customer’s design on the board. Since LMOS closed, these are no longer being manufactured either. There is a large die bank from which parts are being assembled and sold.

## Slide 14: PAL Architecture
Impact Architecture
  50BP70
  OI
  AS ALS F
TiW Fuse Links
Lots of Zener Diodes

## Slide 15: Device Operation / Function
Dr. Jekyll and Mr. Hyde
PALs are really two devices in one package. Under one set of forcing conditions they act one way; under another set of forcing conditions they act another way.

## Slide 16: Programming Mode
When programming a PAL device a set of unique voltage levels are applied to the pins. This causes the device to operate completely different than in operational mode.

## Slide 17: Programming Mode (Con’t)
# Fuses = #Input Lines X #Product Lines

## Slide 18: Programming Mode (Con’t)
Notes: 07/29/26
<number>

## Slide 19: Programming Mode (Con’t)
To blow fuse # 814:
  Select Input Line #13 and Product Line #26.
  This requires the programming configuration for Product Lines 0 - 31

## Slide 20: Programming Mode (Con’t)
To blow fuse # 814 the following configuration results:

## Slide 21: Programming Mode (Con’t)

## Slide 22: Programming Mode (Con’t)
A simplified programming circuit is shown here.

## Slide 23: Programming Mode (Con’t)
These algorithms could be fairly difficult to execute without some pretty sophisticated equipment.
Companies like Data I/O specialize in programming integrated circuits. TI supplies them with the algorithms for each device and Data I/O adds the new algorithms to their latest software releases.
These same algorithms can also be easily accomplished on our automatic test equipment.

## Slide 24: Operational Mode
In operational mode, the logic looks very much like a standard bipolar logic device.
One can design anything from a simple inverter to some very complex state machines.
The simplicity of this method is still very popular and there are many competitors designing some very low-power, high-speed, CMOS PALs.

## Slide 25: PAL Programming & Issues
Fusing
  Structures
  Chip Array Layout
  Physical Dimensions
    Fuses
    Transistors
    Zeners
  Time to Fuse
  Waveforms
  Fusing Mechanisms
  Major Contributors to Poor Fusing

## Slide 26: PAL Fusing -- Structures
TI PALs use TiW fuse links. TiW provides a unique fusing scenario that is more reliable. It is also less susceptible to “grow back” via electromigration.
The fuse link looks like a bow tie. This was determined to be the best geometry for optimal fusing results.

## Slide 27: PAL Fusing -- Chip Array Layout

## Slide 28: PAL Fusing -- Chip Array Layout
The actual fuse array is not equal to the datasheet fuse map.
The product lines and input lines are arranged for optimal device functionality not simplicity of diagnostics.

## Slide 29: PAL Fusing -- Chip Array Layout

## Slide 30: PAL Fusing -- Fuse Dimensions
Fuse Target Width is 1.0 um +/- 0.2um.
Fuse Thickness is 400  +/- 100 
Fuse Resistance should be 65

## Slide 31: PAL Fusing -- Time to Fuse
The correct fusing of a circuit is easily determined by looking at a plot of the fuse current vs. time, called Time-To-Fuse (TTF).

## Slide 32: PAL Fusing -- Time to Fuse (Con’t)
Bad Fuse
Good Fuse

## Slide 33: PAL Fusing -- Mechanisms
There is an optimum fusing power. Underblow is produced by too little, and overblow is produced by too much.
The power is somewhere in the range of 45 to 150 mW. If the fusing resistance becomes too large, then the power delivered to the fuse link is marginal and the fuse ends up being leaky because of filaments remaining across the gap.
A “good” blow takes more power, less time to fuse, and thus less total energy.

## Slide 34: PAL Fusing -- Mechanisms (Con’t)
There are three stages to the fusing process
1st Stage -- Before Heat Dissipates
  When the power is first applied, the temperature at the fuse neck rises rapidly.
  No heat is dissipated for the first 50ns or so.
  The temperature rises most rapidly where the power density is the greatest. The temperature reaches about 2/3 the melting point of TiW.
  The dielectrics surrounding the fuse probably do not begin to flow.

## Slide 35: PAL Fusing -- Mechanisms (Con’t)
2nd Stage -- Heat Dissipates
  After about 50 ns the link neck temperature continues to rise nearly to the melting point of TiW.
  Heat begins dissipating rapidly in the two lateral directions parallel to the current flow.
  The rate of the temperature rise begins to decrease.
  The dielectric near the neck begins to flow.

## Slide 36: PAL Fusing -- Mechanisms (Con’t)
2nd Stage -- Heat Dissipates
  If the fuse is misaligned or the neck is too large, heat will be removed much more rapidly from one side of the fuse than the other. This movement of the peak temperature point starts before the neck melts and separates.
  In many cases, the neck partially melts and the TiW does not separate, but coalesces into a sphere which remains at the neck and forms what looks like a tonsil from a top view.

## Slide 37: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing
  The peak temperature point stops moving. This happens at a wider point in the link instead of at the smallest point.
  The link does not fuse immeditately but sizzles for a while until there is enough heat to open the entire width of the link.
  Due to the hovering of the peak temperature point, the maximum melting of the bottom dielectric occurs at that spot.
  This point is also the maximum mixing point of Ti, W, Si, O, and N. This region also forms a cavity due to vaporization.

## Slide 38: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  It is doubtful that the TiW alloy maintains its alloy composition throughout the fusing process. It is possible that at around 3100C the Ti will separate from the W because of zone refining (heat + electric field) that is taking place. W will be a solid with a melting point of 3422C.
  At 700C to 1000C, W is stable in contact with SiO2 whereas Ti reacts with it to form oxides and silicides. Similar behavior is expected at higher temperatures. So, W is expected to remain unreactive when in contact with molten SiO2 (liquid at 1700C) while Ti is expected to react to form TiO2.

## Slide 39: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  If rapid cooling takes place then the result ought to be a heterogeneous glass with spheroids of TiO2 and W embedded in it.
  The darker spheres that can be seen are probably W spheroids.

## Slide 40: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  An abrupt irreversible rise in resistance immediately prior to fusing is seen on the waveforms. The abrupt rise in resistance is due to the onset of electromigration. The last decrease in resistance may be due to the refining of W at the neck which will drop its resistivity.

## Slide 41: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  The region from the neck to the peak temperature point probably remains electrically conductive. But the TiW is open in patches in this region.
  The cavity region is almost always off the midpoint of the link favoring the direction of the emitter. This is true because when the link is at or near the melting point, electromigration progresses in the direction of the electron flow -- toward the emitter.

## Slide 42: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  If the W remains largely unreactive, it should have a large surface tension which will be the driving force for breaking the fuse. It appears that both vaporization and melting occur during fusing.
  The fuse melts at the neck but does not vaporize until the maximum temperature point moves off center. When it stops moving, enough heat can be generated in one spot to cause vaporization and the resulting void. Then the fuse breaks.

## Slide 43: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  Fusing cannot occur without a void. Assuming that all the materials expand upon melting, there is no place for it to go.
  Whichever material has the lowest vapor pressure partially vapaorizes, creating a bubble in the liquid TiO2 /W/SiO2 mixture. This allows the surface tension to wick the molten W back and break the fuse.
  As the alloy melts, the liquid sheet will attempt to assume a shape which will minimize the surface tension. As a result, the sheet will draw up into a cylindrical filament. Because of the compressive forces in the area, it will be more like an ellipsoidal cylinder.

## Slide 44: PAL Fusing -- Mechanisms (Con’t)
3rd Stage -- Fusing Details
  If the link neck is too wide you will see two of these cylinders in parallel.
  As the length of the filament increases it becomes unstable and at some critical length it tends to form a large sphere.
  If the sphere is incompletely formed, it remains attached on one side (always opposite the emitter) and takes on the appearance of a tonsil.

## Slide 45: PAL Fusing - So What?
So what does all this lead to?
There are 4 major contributions to poor fusing results.
  Thickness of the TiW fuse link.
  Minimum distance between metal on either side of the fuse.
  Maximum neck size of the fuse link.
  Centering of the fuse between the metal.

## Slide 46: PAL Fusing - Major Contributors to Poor Fusing
Thickness of the TiW fuse link.
  As TiW thickness increases, the dielectric damage at the blow site increases.
  The damage increases because of the large amount of heat that is conducted away from the fuse blow site to the surrounding dielectric.

## Slide 47: PAL Fusing - Major Contributors to Poor Fusing (Con’t)
Minimum distance between metal on either side of the fuse.
  The short lead spacing on either side of the fuse also contributes to the increased transfer of heat away from the blow site.
  Increased damage to the surrounding dielectric is a direct result of the heat being moved away from the blow site too quickly.

## Slide 48: PAL Fusing - Major Contributors to Poor Fusing (Con’t)
Maximum neck size of the fuse link.
  If the neck is too large, the current density will not be high enough and the fuses will be underblown.
  A neck that is too large often exhibits the double tonsil syndrome.
  Insufficient fusing will leave filaments of TiW, resulting in a leaky fuse.

## Slide 49: PAL Fusing - Major Contributors to Poor Fusing (Con’t)
Centering of the fuse between the metal.
  If the fuse is not centered in between metal leads, heat will be removed much more rapidly from one side than the other.
  This causes the point of voiding to be moved too far from the center of the fuse, increasing the time to fuse and possibly producing leaky fuses.

## Slide 50: PAL Transistors and Zeners
PAL transistors are the same as ALS technology.
The zener diodes on the chip are the gate keepers between programming mode and standard operation mode.

## Slide 51: Device Setup & ATE Testing
Unique Test and Programming Hardware
Device Set-up and Testing

## Slide 52: Device Setup & ATE Testing (Con’t)
Unique Test and Programming Hardware
  The PAL group has two desk-top programming and test units.
    Data I/O Programmer.
    Logue McDonald Tester

## Slide 53: Device Setup & ATE Testing (Con’t)
  Data I/O Programmer
    Provides programming capability and limited testing.
    Provides code verification
    Algorithms for programming and verification are part of the software on the machine
  Logue McDonald
    Desk-top, PC controlled tester used by distributors.
    Generation of test programs and vectors based on a customer’s design.
    Performs DC, AC, and Functional testing.

## Slide 54: Device Setup & ATE Testing (Con’t)
ATE Testing
  Impact used for production testing.
  Devices can be programmed and verified on the Impacts.
  DC, AC, and Functional testing can be performed on both programmed and blank devices.

## Slide 55: Device Setup & ATE Testing (Con’t)
A Data I/O Flow is included in your packet in case you need to use this machine.