Texas Instruments Incorporated

6412 Highway 75 South, MS 805

Sherman, Texas 75090

CD4060B

ESD Testing Data

| SHEREL.03.CD.01001 | CD4060B ESD |  |  |
| --- | --- | --- | --- |
| Device: | CD4060BM | Die Rev: | A | Code: | 50C99.2 |
| Wafer Fab: | SHE | Technology: | CMOS | Fab Process: | CD4K |
| A/T Site: | MEX | Package: | SOIC | Pins: | 16 |

| Test Type | Date Code | A/T Lot# | Die Lot# | Voltage | Qty | Fails |
| --- | --- | --- | --- | --- | --- | --- |
| ESD - HBM | 2CATXHM | 2752262 | 2336067 | 0 Hr | 15 | 0 |
|  |  |  |  | 500 V | 3 | 0 |
|  |  |  |  | 1000 V | 3 | 0 |
|  |  |  |  | 1500 V | 3 | 2 |
|  |  |  |  | 2000 V | 3 | 0 |
|  |  |  |  | 2500 V | 3 | 1 |
| ESD - MM | 2CATXHM | 2752262 | 2336067 | 0 Hr | 15 | 0 |
|  |  |  |  | 50 V | 3 | 0 |
|  |  |  |  | 100 V | 3 | 0 |
|  |  |  |  | 150 V | 3 | 0 |
|  |  |  |  | 200 V | 3 | 0 |
|  |  |  |  | 250 V | 3 | 1 |
| ESD - CDM | 2CATXHM | 2752262 | 2336067 | 0 Hr | 15 | 0 |
|  |  |  |  | 200 V | 3 | 0 |
|  |  |  |  | 500 V | 3 | 0 |
|  |  |  |  | 750 V | 3 | 0 |
|  |  |  |  | 1000 V | 3 | 0 |
|  |  |  |  | 1500 V | 3 | 0 |

The following data is for testing completed during the Reliability Monitor on various part number devices with die fabricated using the same die fabrication process as the subject part number device.  This data is not specific to the subject device.

| Test | Conditions | Quantity Tested | Failures |
| --- | --- | --- | --- |
| AUTOCLAVE | 15 psig, 121 Degrees C,96 Hours | 922 | 0 Top of Form |
| HAST | 130 Degrees C / 85 % RH with bias,96 Hours | 1386 | 0 Top of Form |
| LIFE TEST | 125C,1000 Hours | 1057 | 0 Top of Form |
| LIFE TEST | 150C,300 Hours | 463 | 0 Top of Form |
| LIFE TEST | 150C,500 Hours | 2086 | 0 Top of Form |
| TEMP CYCLE | -65 / +150 Degrees C,1000 Cycles | 301 | 0 Top of Form |
| THERMAL SHOCK | -65 / +150 Degrees C,1000 Cycles | 924 | 0 Bottom of Form Bottom of Form Bottom of Form Bottom of Form Bottom of Form Bottom of Form |

Use Disclaimer:

Plastic encapsulated TI semiconductor devices are not designed and are not warranted to be suitable for use in some military applications and/or military environments. Use of plastic encapsulated TI semiconductor devices in military applications and/or military environments, in lieu of hermetically sealed ceramic devices, is understood to be fully at the risk of the buyer.

Quality and Reliability Data Disclaimer:

TI assumes no liability for applications assistance or customer product design. Customers are responsible for their products and applications using TI components. To minimize the risks associated with customer products and applications, customer should provide adequate design and operating safeguards.

Quality and reliability data provided by Texas Instruments is intended to be an estimate of   product performance based upon history only. It does not imply that any performance levels reflected in such data can be met if the product is operated outside the conditions expressly stated in the latest published data sheet for a device.  Device attributes listed in qualification reports may not reflect materials or processes currently being used in the construction of the devices.

Reliability data shows characteristic failure mechanisms of the specific environmental stress as documented in the industry standards for each stress condition.

TI warrants its devices as per datasheet limits.  Any usage outside of these limits is the sole responsibility of the consumer and voids all warranties and responsibilities from TI.

THIS INFORMATION SHOULD NOT BE USED TO ASSIST IN THE PRACTICE OF “UPRATING” OR “UPSCREENING” DEVICES FOR USE BEYOND THEIR RATED LIMITS.