Board Level Reliability (BLR) of LM65645-Q1 “Cobra” device in 20-pin RZT QFN package has been assessed by using the BLR Temperature Cycle (TC) test data of a 20-pin RZT QFN daisy chain package with the same bill of material (BOM) and similar silicon die size.

LM65645-Q1 “Cobra” device in 20-pin RZT QFN Package:

BLR TC Test Data of 20-pin RZT QFN Daisy Chain Package:

| Parameter | Value |
| --- | --- |
| Test Method | Per IPC-9701 standard |
| Board Material | High Tg FR4 |
| Board Thickness (mm) | 1.6 |
| Number of Copper Layers | 8 |
| Solder Paste | SAC305, Lead-free, No Clean |
| Min. Temperature (oC) | -40 |
| Max. Temperature (oC) | 125 |
| Number of Cycles per Hour | 1 |
| Dwell Time (minutes) | 15 |
| Cycle Time (minutes) | 60 |
| Sample Size (units) | 32 |
| Definition of Failure | Daisy chain resistance being higher than 1000 ohm |
| Number of Failed Samples | 19 |
| Number of Non-Failed Samples | 13 |
| Number of Cycles Completed | 6533 |
| Cycles to First Failure | 4814 |
| Characteristic Life (at 63.2% failure rate, Cycles) | 6519 |
| Shape Parameter (Slope) | 11.6 |

| Weibull Plot |  |
| --- | --- |

IMPORTANT NOTICE AND DISCLAIMER

TI PROVIDES TECHNICAL AND RELIABILITY DATA (INCLUDING DATASHEETS), DESIGN RESOURCES (INCLUDING REFERENCE DESIGNS), APPLICATION OR OTHER DESIGN ADVICE, WEB TOOLS, SAFETY INFORMATION, AND OTHER RESOURCES “AS IS” AND WITH ALL FAULTS, AND DISCLAIMS ALL WARRANTIES, EXPRESS AND IMPLIED, INCLUDING WITHOUT LIMITATION ANY IMPLIED WARRANTIES OF MERCHANTABILITY, FITNESS FOR A PARTICULAR PURPOSE OR NON-INFRINGEMENT OF THIRD PARTY INTELLECTUAL PROPERTY RIGHTS.

These resources are intended for skilled developers designing with TI products. You are solely responsible for (1) selecting the appropriate TI products for your application, (2) designing, validating and testing your application, and (3) ensuring your application meets applicable standards, and any other safety, security, or other requirements. These resources are subject to change without notice. TI grants you permission to use these resources only for development of an application that uses the TI products described in the resource. Other  reproduction  and  display  of  these  resources  is  prohibited.  No  license  is  granted  to  any  other  TI intellectual property right or to any third party intellectual property right. TI disclaims responsibility for, and you will fully indemnify TI and its representatives against, any claims, damages, costs, losses, and liabilities arising out of your use of these resources.

TI’s  products  are  provided  subject  to  TI’s  Terms  of  Sale  (www.ti.com/legal/termsofsale.html) or  other applicable terms available either on ti.com or provided in conjunction with such TI products. TI’s provision of these resources does not expand or otherwise alter TI’s applicable warranties or warranty disclaimers for TI products.