TI qualification testing is a risk mitigation process that is engineered to assure device longevity in customer applications.  Wafer fabrication processes and package level reliability are evaluated in a variety of ways that may include accelerated environmental test conditions with subsequent derating to actual use conditions. Manufacturability of the device is evaluated to verify a robust assembly flow and assure continuity of supply to customers.  TI commercial Products are qualified with industry standard test methodologies performed to the intent of Joint Electron Devices Engineering Council (JEDEC) standards and procedures.  .

Qualification by Similarity (Qualification Family)

A new device can be qualified either by performing full scale quality and reliability tests on the actual device or using previously qualified device(s) through "Qualification by Similarity" (QBS) rules. By establishing similarity between the new device and those qualified previously, repetitive tests will be eliminated, allowing for timely production release.  When adopting QBS methodology, the emphasis is on qualifying the differences between a previously qualified product and the new product under consideration.  The QBS rules for a technology, product, test parameters or package shall define which attributes are required to remain fixed in order for the QBS rules to apply. The attributes which are expected and allowed to vary will be reviewed and a QBS plan shall be developed, based on the reliability impact assessment above, specifying what subset of the full complement of environmental stresses is required to evaluate the reliability impact of those variations. Each new device shall be reviewed for conformance to the QBS rule sets applicable to that device.   See JEDEC JESD47 for more information.

| Device Baseline |  |  |  |  |
| --- | --- | --- | --- | --- |
| TI Device: | LMZ14202EXTTZ/NOPB LMZ14202EXTTZE/NOPB LMZ14202EXTTZX/NOPB | Small T&R Tube Large T&R | Pin/Package Type: | 7TO-PMOD |

| TI Commercial Products New Device Qualification Matrix |  |  |  |  |
| --- | --- | --- | --- | --- |
| Note that qualification by similarity (“qualification family”) per JEDEC JESD47 is allowed |  |  |  |  |
| Description | Condition | Sample Size (Used/Rejects) | Lots Required | Test Method |
| Electrostatic Discharge Sensitivity | HBM : 2000V | 3 /0 3/0 | 1 | EIA/JESD22-A114 |
|  | CDM: 500V |  |  | EIA/JESD22-C101 |
| Latch-up | 25C, 125C | 6/0 | 1 | EIA/JESD78 |
| Bias Life Test | 150°C / 408 hours or equivalent | 77/0 | 3 | JESD22-A108 |
| Biased HAST | 110°C / 85% / 264 hours | 77/0 | 3 | JESD22-A110* |
| Temperature Cycle | -40°C to +125°C non-biased for 1000 cycles | 77/0 | 3 | JESD22-A104* |
| High Temp Storage | 150 °C / 1,000 hours | 77/0 | 3 | JESD22-A103-A |
| Additional testing for “EXT” |  |  |  |  |
| Temperature Cycle | -55°C to +125°C non-biased for 1000 cycles | 77/0 | 1 | JESD22-A104* |
| Power Temp Cycle | -55°C to +125°C biased for 1000 cycles | 77/0 | 1 | JA105 |
| Vibration | JESD22-B103B condition 1 and MIL-STD-883 Method 2007.2 Condition A. | 77/0 | 1 | JESD22-B103B condition 1 and MIL-STD-883 Method 2007.2 Condition A. |
| Mechanical shock | JESD22-B110 condition B and MIL-STD-883 Method 2002.3 Condition B. | 77/0 | 1 | JESD22-B110 condition B and MIL-STD-883 Method 2002.3 Condition B. |
|  | *Precondition performed per JEDEC Std. 22, Method A112/A113 |  |  |  |

For additional information or technical support please Email TI

Important Limitations on Use of Data Exceeding Specified Limits

TI is providing this data for your convenience. However, we want to make clear the significant limitations of its usefulness as an indicator of how devices may perform in various applications.

THIS DATA IS PROVIDED "AS IS" WITHOUT ANY EXPRESS OR IMPLIED WARRANTY OF ANY KIND INCLUDING WARRANTIES OF MERCHANTABILITY, NONINFRINGEMENT OF INTELLECTUAL PROPERTY, OR FITNESS FOR ANY PARTICULAR PURPOSE. IN NO EVENT SHALL TI OR ITS SUPPLIERS BE LIABLE FOR ANY DAMAGES WHATSOEVER (INCLUDING, WITHOUT LIMITATION, DAMAGES FOR LOSS OF PROFITS, BUSINESS INTERRUPTION, LOSS OF INFORMATION) ARISING OUT OF THE USE OF OR INABILITY TO USE THE INFORMATION, EVEN IF TI HAS BEEN ADVISED OF THE POSSIBILITY OF SUCH DAMAGES.

Your use of this data, and all consequences of such use, is solely your responsibility. You must perform sufficient engineering and additional qualification testing in order to properly evaluate your application and determine whether a candidate device is suitable for use in that application.

TI semiconductor components are specifically designed and manufactured to be used within the electrical, thermal, mechanical and other parameters set forth in TI's product data sheets. Quality and reliability data provided by Texas Instruments, such as MTBF and fit rate data, is intended to be an estimate of product performance based upon history only. It does not imply that any performance levels reflected in such data can be met if the product is operated outside the conditions expressly stated in the latest published data sheet for a device.

Plastic encapsulated TI semiconductor devices are neither designed nor warranted as suitable for use in military applications and/or military environments.

THIS INFORMATION SHOULD NOT BE USED TO ASSIST IN THE PRACTICE OF "UPRATING" OR "UPSCREENING" DEVICES FOR USE IN MILITARY OR OTHER CRITICAL APPLICATIONS. There are significant limitations of this information as an indicator of how commercial, off-the-shelf (COTS) devices may perform in such applications or environments, and about the hazards of using COTS devices in such applications. TI strongly believes that semiconductor components should never be used outside their specified tolerance levels as up-screening can lead directly to system or component failure. Such failures may present distinct risks to end-users and to third parties. TI cannot accept any responsibility for component or system failures that occur due to the misuse of its products, including misuse that may result from the practice of up-screening.

Any use of TI components beyond their rated limits voids all warranty responsibility of TI with respect to such devices, and also voids all responsibility of TI with respect to any applications assistance, product design, software performance or services of any kind that were or may have been performed in connection with the sale of any such devices. Further, resale of TI's products or services with statements different from or beyond the parameters stated by TI for that product or service in official TI data books or data sheets, or without the warnings or instructions provided by TI, voids all express and any implied warranties for the associated TI product or service, and is an unfair and deceptive business practice.